Fig. 1. Vector, basis, relative basis.

a  the vector as a physical object, invariant to the co-ordinate system chosen; b  the a-vector and its oblique projections ai onto the directions of the basis ei; c – relative basis.

Fig. 2. Covariant, orthogonal, ( a1, a2) and contravariant, oblique, (a1, a2) projections of the a-vector

a                                                     b

Fig. 3. A fixed, e.g. Cartesian, system of reference xi (a); a convected, Lagrangian, co-ordinate system yi (b).

Fig. 4. Velocity field in the neighbourhood of point Ì  the centre of an infinitesimal continuum particle, Ì' being an arbitrary point of the neighbourhood.

Fig. 5. An elementary tetrahedron and surface stresses on its facets  related by Eq. (63)

Fig. 6. Plasticity testing in a pressurised liquid: torsion (a), tension (b)

Fig. 7. The diagrams Λр=Λрk1 for the alloys 08Kh18N10T (a), 12Kh1MF (b) and the aluminium alloy AD-1 (c) obtained in torsion (curves 1, k2=0) and in tension (curves 2, k2=−1), and the diagram a=ak1 for some steels (d) obtained in torsion (k2=0): 1  steel 08Kh18N10T, 2  steel St45, 3  steel Shkh15 (transliterated standard Russian nomenclature of steel grades and alloys is used hereinafter in Part II)

Fig. 8. Slip-line network near a cut made in a wide prismatic specimen under bending

Fig. 9. Plasticity diagram for quenched and tempered rail steel when k2=0

a

b

d

c

Fig. 10. The microstructure of St3sp steel specimens with different calculated ψ (the photographs were made by the JSM-V3 scanning electronic microscope with an 15000 magnification): ψ=0.00 (a); ψ=0.45 (b); ψ=0.75 (c); ψ=1.00 (d).

Fig. 11. The density of steel St3sp as a function of damage resulting from plastic deformation

Fig. 12. Experimental results (dots) and predicted damage curve in two-stage deformation (tension and torsion) to fracture.

Fig. 13. Plasticity as a function of the logarithm of strain rate for molybdenum (a) and titanium (b) under liquid pressure p = 0.1 MPa (1), 200 MPa (2), 500 MPa (3) and 800 MPa (4)

Fig. 14. A decrease in metal damage (steels 12Kh18N10T, St3sp and titanium alloy VT1-0) from plastic deformation, which results from recrystallization annealing. Line 1  when hydrostatic pressure is imposed during thermal treatment

Fig. 15. Variation of damage from plastic deformation for steel 20 in thermal treatment at 600С: 1  ψ1= 0; 2  0.2; 3  0.6; 4  0.7

Fig. 16. A macroscopic elementary volume of a body under deformation. Microscopic objects are metal grains or crystallites; submicroscopic objects are discontinuities (short irregular lines) in the grains.

- Fig.17. Construction to prove some basic theorems.

- Fig. 18. A bar impinging on a rigid target

Fig. 19. The variation-difference solution. Node displacement

- Fig. 20. Solution with Fourier series. Stresses

- Fig. 21. Damage along an elastic bar

- Fig. 22. The instant of the first fracture as dependent on bar velocity

- Fig. 23. The co-ordinates of the point of the first fracture as dependenton the bar velocity

- Fig. 24. The displacement of the fracture point

Fig. 26. Hammer forging: 1  top die head, 2  forging, 3  bottom die head with an anvil

Fig. 27. To the calculation of the stress-strain state in parallelepiped forging

Fig. 28. The distribution of mean normal stress  (Pa) in the section  y3= 0.05 early (a) and late (b) in upsetting

Fig. 29. The variation of  (Pa) with time in the parallelepiped centre, with the die head mass to parallelepiped mass ratio: 1  712251; 2  178063; 3  17806

Fig. 30. An implosive accelerator: 1  detonator,  2  explosive charge, 3  facing, 4   Al2O3 powder

Fig. 31. To Grigoryan’s model of superdeep penetration: a  section along the particle motion path; b  cross section

Fig. 32. To the determination of particle penetration depth: a  ordinary case, b  superdeep penetration under favourable conditions for fracture, e.g., due to the wave process in the target, 1  target, 2  particle