Fig. 59. Penetration mechanisms and geometry for projectile-target system [137]

Region 1 - rigid projectile, region 2 - deformed portion of plug, region 3 - outer target zone deformed by plastic hinge, region 4 - undeformed plug region, region 5 - undeformed outer target zone, I - plastic shock layer in target, II - plastic hinge

Fig. 60. Computed force histories for the normal penetration of a 6.4 mm thick 2024-0 aluminium plate struck by a rigid projectile at velocities ranging from 1 to 10 times the plate's ballistic limit [137]

Fig. 61. Velocity ratios V1V0, V3V0, V4V0 for the penetration of a 6.4 mm thick 2024-0 aluminium plate by a rigid projectile

Solid lines represent an impact velocity, V0=104 m/s (V0Vx=1); dashed lines represent V0=1040 m/s (V0Vx=10), lower axis t. V1,V3 and V4are as defined in Ref. [137]

Fig. 62. Residual velocity as a function of initial velocity predicted by three perforation models for the impact of a 7.32 g hard steel cylinder with a diameter of 7.82 mm striking a 6.35 mm thick aluminium plate [137]

1 - Recht and Ipson [32], 2 - Heyda et al [138], 3 - Liss et al [137]